## Slide 1
Interface-sensitive
optical tenique
PCE
hole transfer rate
-(CH2)nCH3
P3DDT
12
P3BT
P3HT
P3OT
P3DT
N= 4
6
8
10
Side Chain length
Short
Long
SFG
Hole trans-
fer rate
Influence of Alkyl Side-chain Structure on
Charge Transfer Rate
Chuanzhao Li , Yi Luo, Shuji Ye*
University of Science and Technology of China
Hefei National Laboratory for Physical Sciences at Microscale，230026，Hefei
E-mail: shujiye@ustc.edu.cn
Introduction
wIR+ wvis = wsfg
Experiment Content
Acknowledgements
National Natural Science Foundation of China (Grants 21473177, 91127042)
Fundamental Research Funds for the Central Universities(WK2340000064)
Key Research Program of the Chinese Academy of Sciences
Summary
1. Alkyl side-chains introduce two competing effects: the steric hindrance and the intermolecular dispersive attraction (Marcus theory).
2.
require
hole and electron separation and recombination occurs at the interfaces
How to precisely describe interacial molecular
structure?
How to build the relationship between structure
and perfomance?
Molecular
structure
Effect of peripheral groups on the PCE
Effect of molecular symmetry on the PCE
Effect of functional groups density on the PCE
Mainly focus on pursuing the better performance
Previous studies
The steady state and time-resolved PL spectrum of perovskite/P3ATs heterojunctions
Figure 1 A)Steady state PL spectrum B) Time-resolved PL spectrum
Figure 1 A) :The steady state PL spectrum of Perovskite/P3ATs heterojunctions.
Figure 1 B): The time-resolved PL spectrum of Perovskite/P3ATs heterojunctions.
The side-chain molecular order of P3ATs is different.
Figure 2 A):The ssp SFG spectrum of P3ATs.
Figure 2 B): After fitting Figure 2 A), the value of CH2,ss/CH3,ss
SFG spectrum of P3ATs
Hole-extraction capability of P3ATs from perovskite layer is different.
The connection between side-chain molecular order of P3ATs and the hole-extraction capability
The side-chain molecular order of P3ATs is consistent with
hole extraction capability.
The schematic representation of
chain arrangements in P3BTand P3HT
Figure 4. The schematic representation of chain arrangements in P3BT and P3HT according to previous results of GIXRD.
P3ATs
PVSK
h+
Figure 2A) The ssp spectrum of P3ATs
B) The value of CH2,ss/CH3,ss
Figure 3. Red line is the value of CH2,ss/CH3,ss, black line is the ratio between PL intensity of heterjunction and that of pure perovskite.
0.379nm
~2 nm
~2 nm
0.386nm
ΔG ±
ΔG 0
Invesion area
Normal area
SFG
Steric constraints
'Trans' or 'gauche'
Long range molecular order
Hole transfer rate
Π-stacking distance is not the main reason